METALITH – EC (Erosion Control)

METALITH – EC is a prefabricated aluminum “bin type” revetment system which is ideally suited for the prevention of topsoil erosion and the stabilization of riverbanks and streams.  METALITH – EC is comprised of only two components:

- .063” thick aluminum panels perforated with 216 ¾” holes per lineal foot of perforated panel

- Type 419 stainless steel connecting pins

The system is assembled on site by connecting the aluminum panels together with the connecting pins to form a series of “bins” which are then filled with rock and/or gravel.

This is a 100% RE-USEABLE product which is also 100% GREEN